Hellenic Accreditation System

| Annex F1/14 to the Certificate No. 754-3 SCOPE of ACCREDITATION of KAPOGIANNI DOMOEREVNA IKE Quality Control Laboratories Concrete-Aggregate-Soil Mechanics and Asphalt Testing |
| --- |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| Physical & Chemical Testing |
| Hardened Concrete | Testing hardened concrete-Part 2: Making and curing of test specimens (15cm x 15cm x 15cm) for strength tests | ELOT ΕΝ 12390-2: 2019 |
| Aggregates | 1.Tests for general properties of aggregates - Part 2: Methods for reducing laboratory samples | ELOT ΕΝ 932-2: 2000 |
|  | 2.Tests for geometrical properties of aggregates - Part 1: Determination of particle distribution – Sieving method | ELOT ΕΝ 933-1: 2012 |
|  | 3.Tests for geometrical properties of aggregates - Part 8: Assessment of fines – Sand equivalent test | ELOT ΕΝ 933-8: 2015 |
|  | 4.Tests for geometrical properties of aggregates - Part 9: Assessment of fines – Methylene blue test | ELOT ΕΝ 933-9+Α1: 2014 |
|  | 5. Tests for mechanical and physical properties of aggregates - Part 6: Determination of particle density and water absorption. | ELOT ΕΝ 1097-6 :2013 |
|  | 6. Tests for mechanical and physical properties of aggregates - Part 3: Determination of loose bulk density and voids. | ELOT ΕΝ 1097-3: 1999 |
|  | 7. Tests for thermal and weathering properties of aggregates. Part 2 : Magnesium sulfate test | ΒS EN 1367-2 : 2009 |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Bituminous mixtures | 1. Test methods for hot mix asphalt Part 1: Soluble Binder Content | ΕΝ 12697-1 : 2020 |
|  | 2.Test methods for hot mix asphalt – Part 2: Determination of particle size distribution | ΕΝ 12697-2 : 2019 |
| Soils | Standard test method for In Place Density and Water Content of Soil and Soil-Aggregate by Nuclear Methods (Shallow Depth) | ASTM D 6938-17a |
| Mechanical Testing |
| Hardened Concrete | 1.Testing concrete in structures. Part 1: Cored specimens. Taking, examining and testing in compression | ELΟΤ ΕΝ 12504-1: 2020 |
|  | 2.Testing hardened concrete. Part 3: Compressive strength of test specimens | ELΟΤ ΕΝ 12390-3: 2019 |
| Aggregates | Tests for mechanical and physical properties of aggregates- Part 2: Methods for the determination of resistance to fragmentation in the Los Angeles machine | ELOT EN 1097-2: 2020 |

Site of assessment: Permanent laboratory premises, 82-84, Evangelistrias Str., Kallithea, Attiki, Greece.

Approved Signatories: Kapogiannis George, Kapogianni Chryssoula, Efthymiou Charalabos.

This Scope of Accreditation replaces the previous one dated  03.01.2024.

The Accreditation Certificate No. 754-3,  to ELOT EN ISO/IEC 17025: 2017, is extended until 03.05.2024.

Athens, 01.03.2024

Christos Nestoras

CEO of ESYD