Hellenic Accreditation System

Annex F1/A22 to the Certificate No. 47-7 SCOPE of ACCREDITATION of the Testing Laboratories of the General Applications of Technology and Science Ltd., GATS SINGLE MEMBER LIMITED LTD. (Laboratory in Athens)

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Weldings of metal structures Weldings of metal structures (cont.) | 1. Radiography testing | ASME V-art2: 2021 ASME IX QW-191.1: 2021 ASME VIII-art5/7-app.4/6/7: 2021 API 1104 §11.1: 2021 EN ISO 5817: 2014 EN ISO 17636-1: 2013 EN ISO 10893-6: 2019 |
|  | 2. Ultrasonics testing - Welding test (conventional method) - Phased Array Method - Thickness measurements | ASME V-art4/5: 2021 ASME IX QW-191.2: 2021 ASME VIII-app.6/12: 2021 API 1104 §11.4: 2021 EN ISO 5817: 2014 EN ISO 17640: 2018 BS EN ISO 23279: 2017 EN ISO 13588: 2019 ASME V-art23/Appx IV,V: 2021 ΕΝ 10160: 1999 EN ISO 16809: 2019 |
|  | 3. Magnetic particles testing using portable electromagnet (YOKE) | ASME V-art7: 2021 ASME VIII-art7-app.6/7: 2021 API 1104 §11.2: 2021 EN ISO 5817: 2014 ELOT EN ISO 17638: 2016 |
|  | 4. Liquid penetrants testing and fluorescent portable equipment | ASME V-art6: 2021 ASME IX QW-195.1: 2021 ASME VIII-art6-app.7/8: 2021 API 1104 §11.3: 2021 EN ISO 5817: 2014 EN ISO 3452-1: 2021 BS EN ISO 10893-4: 2011 |
|  | 5. Visual testing | ASME V-art 9: 2021 ASME IX QW-194: 2021 EN ISO 5817: 2014 ELOT EN ISO 17637: 2016 |
|  | 6. Macroscopic Examination | ASME IX: 2021 – QW 183, QW 184 EN ISO 17639: 2013 PD CEN ISO/TR 16060: 2014 ASTM E340-15 |
| Metallic materials and products | 2. Bending testing Athens: (0 - 500) kN | ASME IX QW-160: 2021 API 1104 §5.6.4-5.6.5/6.5: 2021 ELOT EN ISO 5173: 2011+Α1/2012 |
|  | 3.Visual examination of defects following destructive testing | ASME IX QW-183/184: 2021 |

Site of assessment :  Laboratory permanent premises, 156 Karamanli Ave., Acharne, Athens, Greece.

Approved signatories : G. Fyrigos, C. Molfesis, Ε. Savopoulos, G. Vlachos,  Th.Karaiskos, P.Vanias (Non-destructive tests).G. Fyrigos, Ε. Pouleas, A. Strantzas (Mechanical tests).

This Scope of Accreditation replaces the previous one dated May 23rd, 2022.

The Accreditation Certificate No. 47-7, to ELOT EN ISO/IEC 17025: 2017, is valid until 26.11.2025.

Athens, July 27th, 2022

Christos Nestoras

CEO of ESYD

# Text boxes

Non-destructive material tests

###### Mechanical tests