Hellenic Accreditation System

| Annex F1/12 to the Certificate No.646-5 SCOPE of ACCREDITATION of the «Standard Chemical Laboratory of Northern Greece» οf the P.P.C. S.A. |
| --- |
| Materials / Tested products | Type of test/ Measured properties | Applied standards/ Techniques used |
| Chemical Testing |
| Solid Fossil Fuels | Proximate analysis / Determination of moisture, ash and volatile matter by instrumental procedures | ASTM D 7582 -2015 Standard Test Methods for Proximate Analysis of Coal and Coke by Macro Thermogravimetric Analysis |
|  | Gross Calorific Value of Coal and Coke / Determination of Gross and calculation of Net calorific value by isoperibol or adiabatic bomb calorimeter | ASTM D 5865-2019 Standard Test Method for Gross Calorific Value of Coal and Coke |
|  | Elemental analysis / Instrumental determination of Carbon, Hydrogen and Nitrogen | ASTM D 5373-2021 Standard Test Methods for Instrumental Determination of Carbon, Hydrogen, and Nitrogen in Laboratory Samples of Coal |
| Solid Fossil Fuels | Determination of sulfur content. | ASTM D4239-2018e1 Standard Test Method for Sulfur in the Analysis Sample of Coal and Coke Using High-Temperature Tube Furnace Combustion DIN 51724-3/12 Solid mineral fuels - Determination of sulfur content - Part 3: Instrumental methods |

Site of assessment: Laboratory permanent premises, SCLNG / Withdrawal Preparation Sector of Kardia, 14th km Kozani – Ptolemaida, 50200 Greece.

Approved signatories: Christina Chatzifoti, Andreana Siakavara

This scope of Accreditation replaces the previous one dated 23.12.2021.

The Accreditation Certificate No.646-5 to ELOT EN ISO/IEC 17025:2017, is valid until 17.12.2025.

Athens, 06.07.2023

Christos Nestoras

CEO of ESYD