Hellenic Accreditation System

| Annex F1/1 to the Certificate No. 1200 SCOPE of ACCREDITATION of the Testing Laboratory of ‘‘G. KARYDIS - DOMO+LYSISLAB – Laboratory of Structural Assessment and Protection’’ |
| --- |
| Tested Materials / Products | Types of Test / Properties to be measured / Procedures | Applied Standards / Techniques to be used |
|  | Non-Destructive Testing |  |
| Hardened Concrete | Testing concrete in structures. Non-destructive testing. Determination of rebound number | EN 12504 - 2: 2012 |
|  | Testing concrete. Determination of ultrasonic pulse velocity | EN 12504 - 4: 2004 |
| Metals / Concrete | Testing concrete. Recommendations on the use of electromagnetic cover meters. | BS 1881 - 204: 1988 |
|  | Standard test method for corrosion potentials of uncoated reinforcing steel in concrete. | ASTM C 876 – 15 (2015) |
| Coatings – Lining Systems | Determination of the film thickness of coatings using an ultrasonic gage. | ISO / TS 19397: 2018 |
| Tested Materials / Products | Types of Test / Properties to be measured / Procedures | Applied Standards / Techniques to be used |
|  | Physical Testing |  |
| Coatings – Lining Systems | Wedge – cut method for determination of film thickness (Scribe and Drill method) | EN ISO 19399: 2016 Method Α (Scribe) Testing only on site. Does not comply with §7, §8.1 |
|  | Mechanical Testing |  |
| Concrete / Mortars / Cementitious Slurries | Product and systems for the protection and repair of concrete structures – Test methods – Measurement of bond strength by Pull-Off. | EN 1542: 1999 Testing only on site. Does not comply with §2 §4.1, 4.2, 4.3, 4.4, 4.12, §5, §6. |
| Fiber Reinforced Polymers (FRP) Laminates | Standard test method for Pull-Off strength for FRP Laminate systems bonded to concrete substrate. | ASTM D 7522 – 15 (2015) |
| Coatings – Lining Systems | Paints and varnishes. Pull-Off test for adhesion. | EN ISO 4624: 2016 Method Β Testing only on site. Does not comply with §6, §7, §8.1, 8.2 |
|  | Paints and varnishes. Cross-cut test for adhesion. | EN ISO 2409: 2013 Testing only on site, with hand-held cutting tool §3.2.3.1. Does not comply with §4, §5, §6.1.2, 6.1.3, 6.3 |

Site of assessment: Laboratory permanent premises: Distomoy 97 - Kolonos - Athens - 10443, Athens

Approved signatories: Georgios Karydis

The Accreditation Certificate No.  1200  to ELOT EN ISO/IEC 17025:2017, is valid until February 9th, 2020.

Athens, February 10th, 2020

Spyridon Podaras

CEO of ESYD