Hellenic Accreditation System

| Annex F1/16 to the Certificate No. 509-6 SCOPE of ACCREDITATION of the Testing Laboratory of the Department of Materials Quality and Public Works’ Control of Thessaly of the Directorate of Technical Control of the Decentralised Government of Thessaly - Central Greece |
| --- |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| Mechanical tests |
| Concrete | 1.Testing hardened concrete – Part 3: Compressive strength of test specimens | ΕΛΟΤ EN 12390-3:2019 |
|  | 2.Testing concrete in structures Part 1 : Cored specimens Taking, examining and testing in compression | EN 12504-1 : 2019/AC:2020 Concrete Technology Regulation (CTR 2016) |
| Aggregates | Tests for mechanical and physical properties – Part 2: Methods for the determination of resistance to fragmentation (Los Angeles test) | ΕΛΟΤ ΕΝ 1097-2:2020 |
| Bituminous mixtures | Bituminous mixtures - Test methods for hot mix asphalt - Part 34: Marshall test Test methods for hot mix asphalt – Part 30: Specimen preparation by impact compactor | EN 12697-34:2020 ΕΝ 12697-30:2018 |
| Physical and physicochemical tests |
| Aggregates of bituminous mixtures | Test methods for hot mix asphalt – Part 2: Determination of particle size distribution | ΕΝ 12697-2:2015 +A1:2019 |
| Aggregates | 1.Tests for geometrical properties – Part 1: Determination of particle size distribution – Sieving method | ΕΛΟΤ ΕΝ 933-1 : 2012 |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Aggregates | 2. Test for geometrical properties – Part 8: Assessment of fines. Sand equivalent test | ΕΛΟΤ ΕΝ 933-8: 2012 + A1:2015 |
|  | 3.Sand Equivalent Test of Soils and Fine Aggregates | ASTM D2419-2022 |
|  | 4.Tests for mechanical and physical properties of aggregates - Part 6: Determination of particle density and water absorption Parag. 9 Pyknometer method for aggregate particles passing the 4 mm test sieve and retained on the 0,063 mm test sieve | ΕΛΟΤ ΕΝ 1097-06: 2022 |
|  | 5.Tests for geometrical properties of aggregates – Part 9 : Assessment of fines – Methylene blue test | EN 933-9:2022 |
| Aggregates and Soils | 1.Determining the Liquid Limit of Soils | AASHTO T 89-2022 |
|  | 2.Determining the Plastic Limit and Plasticity Index of Soils | AASHTO T 90-2020 |
|  | 3.Standard method for liquid limit, plastic limit and plasticity index | National Specification Ε 105: 1986, Tests 5 & 6 |
| Bituminous mixtures | 1.Bituminous mixtures – Test methods – Part 6: Determination of bulk density of bituminous specimens Procedure A:Bulk density – dry Procedure B: Bulk Density – Saturated surface dry (SSD) | EN 12697-6:2020 |
|  | 2.Bituminous mixtures – Test methods – Part 29: Determination of the dimensions of a bituminous specimen | EN 12697-29:2020 |
| Chemical tests |
| Bituminous mixtures | Test methods for hot mix asphalt – Part 1: Soluble binder content (Extraction method) | ΕΝ 12697-1:2020 |

Site of assessment: Laboratory permanent premises, 28 Tsamadou and Kodringtonos str., 383 34 Volos, Greece.

Approved signatories: Georgios Lekarakos

This Scope of Accreditation replaces the previous one dated 27.01.2023

The Accreditation Certificate No. 509-6, to ELOT EN ISO/IEC 17025: 2017, is valid until 18.02.2025.

Athens, 21.02.2024

Christos Nestoras

CEO of ESYD