Hellenic Accreditation System

Annex F1/2 to the Certificate No. 1285 SCOPE of ACCREDITATION of the Laboratory of the SpectrumNDT – I.Dimoulis Co. Ltd.

| Materials / Products to be tested | Types of test / Properties to be measured | Applied Methods / Techniques to be used |
| --- | --- | --- |
| Non destructive tests |
| Metallic Materials / Welds, Casting, Forgings | 1. Magnetic particle testing by the use of portable electromagnetic equipment (yoke). Examination for surface discontinuities | EN ISO 17638: 2016 Non-destructive examination of welds – Magnetic particle testing of welds ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 7: Magnetic particle examination EN 10228-1: 2016 Non-destructive testing of steel forgings – Part 1: Magnetic particle inspection EN 1369: 2012 Founding – Magnetic particle inspection |
| Metallic Materials / Welds, Casting, Forgings | 2. Liquid penetrant testing Examination for surface discontinuities | EN 10228-2: 2016 Non-destructive testing of steel forgings – Part 2: Penetrant testing ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 6: Liquid penetrant examination EN ISO 3452-1: 2021 Non-destructive testing – Penetrant testing – Part 1: General principles EN 1371-1: 2011 Founding – Liquid penetrant inspection – Part 1: Sand, gravity die and low pressure die castings |
| Metallic materials / Welds | 3. Ultrasonic testing Examination for discontinuities on welds (conventional method) Phased Array Method Thickness measurement | ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 4: Ultrasonic examination methods for in-service inspection. Article 5: Ultrasonic examination methods for materials and fabrication EN ISO 17640:2018 Non-destructive testing of welds – Ultrasonic testing - Techniques, testing levels and assessment ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Articles 4 & 23: Ultrasonic examination methods EN ISO 13588: 2019 Non-destructive testing of welds. Ultrasonic testing. Use of automated passed array technology ASTM E2700: 2020 Standard practice for contact Ultrasonic Testing of welds using phased arrays EN ISO 16809: 2022 Non-destructive testing. Ultrasonic thickness measurement |
| Metallic Materials / Welds | 4. Radiographic inspection | ΕΝ ISO 17636-1: 2013 Non-destructive testing of welds – Radiographic testing – Part 1: X- and gamma-ray techniques with films ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 2: Radiographic examination |
| Metallic Materials / Welds | 5. Visual Examination | ΕΝ ISO 17637: 2016 Non-destructive testing of welds – Visual testing of fusion welded joints ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 9: Visual examination |

Site of assessment: Laboratory permanent premises, Efplias 49, Piraeus, Greece

Approved signatories: I.Dimoulis, Em.Manta, K.Mperketis

This Scope of Accreditation replaces the previous one dated February 18th, 2022.

The Accreditation Certificate No. 1285 to ELOT EN ISO/IEC 17025:2017, is valid until 17.02.2026.

Athens, August 21st, 2023

Christos Nestoras

CEO of ESYD