Hellenic Accreditation System

Annex F1/4  to the Certificate No. 1269

SCOPE of ACCREDITATION of the Testing Laboratory of ‘’EDAFOMICHANIKI S.A. – Laboratory for Soil & Rock Mechanics – Aggregates – Bituminous Mixtures - Concrete.’’

| Tested materials / Products | Types of test / Properties to be measured / Procedures | Applied Standards / Techniques to be used |
| --- | --- | --- |
| Physical testing |
| Soil - Rock | 1. Determination of material finner than Νο200 | Ε 105 – 86 § 8 |
|  | 2. Determination of water content of rock sample | Ε 103 – 84 §1 |
|  | 3. Determination of water content | EN 17892-1:2015 |
|  | 4. Determination of bulk density (Immersion in fluid method) | EN 17892-2:2015 |
|  | 5. Determination of particle density (Fluid pycnometer method) | EN 17892-3:2015 |
|  | 6. Determination of liquid and plastic limit (Fall cone method) | EN 17892-12:2018/A2:2022 |
|  | 7. Determination of particle size distribution (Sieving method & hydrometer method) | EN 17892-4:2016 |
| Soil | Determination of the organic material of peat and other organic soils (Method A) | ASTM D2974:2020 |
| Aggregates | 1. Tests for geometrical properties of aggregates - Part 1: Determination of particle size distribution - Sieving method | ΕΝ 933-1:2012 |
|  | 2. Determination of particle density and water absorption (Annexes A, B, D, F, H, I) | ΕΝ 1097-6:2022 |
| Concrete | Testing hardened concrete - Part 2: Making and curing specimens for strength tests (cubic specimens 15cm x 15cm x15cm) | ΕΝ 12390.02:2019 |

| Tested materials / Products | Types of test / Properties to be measured / Procedures | Applied Standards / Techniques to be used |
| --- | --- | --- |
| Mechanical testing |
| Soil - Rock ΄ | 1. Unconsolidated undrained triaxial test (UU) | EN 17892-8:2018 |
|  | 2. Consolidated triaxial compression tests on water saturated soils (CUPP & CD) | EN 17892-9:2018 |
|  | 3. Preparation of rock core as cylindrical test specimens and verifying conformance to dimensional and shape tolerance | ASTM D4543:2019 |
|  | 4. Compressive strength and elastic moduli of intact rock core specimens under varying states of stress and temperatures (Methods C & D) | ASTM D7012:2023 |
|  | 5. Determination of point load strength index of rock and application to rock strength classifications | ASTM D5731:2016 |
|  | 6. Direct shear tests on remoulded specimens (CD & Ring shear) | EN 17892-10:2018 |
|  | 7. Determination of laboratory reference density and water content with rammer 2.5kg and 4.5kg (Proctor compaction) | EN 13286-2:2010 |
|  | 8. Determination of california bearing ratio, immediate bearing index and linear swelling (CBR) | EN 13286-47:2021 |
|  | 9. Incremental loading oedometer test | EN 17892-5:2017 |
|  | 10. Unconfined compression test | EN 17892-7:2017 |
| Aggregates | 1. Tests for mechanical and physical properties of aggregates - Part 2: Methods for the determination of resistance to fragmentation (Los Angeles test) | ΕΝ 1097-2:2020 |
|  | 2. Tests for geometrical properties of aggregates - Part 3: Determination of particle shape - Flakiness index | ΕΝ 933.03:2012 |
|  | 3. Tests for geometrical properties of aggregates - Part 9: Assessment of fines - Methylene blue test | ΕΝ 933.09:2009 + A1: 2022 |
|  | 4. Tests for geometrical properties of aggregates - Part 8: Assessment of fines - Sand equivalent test | ΕΝ 933.08:2012 + A1:2015 |
|  | 5. Tests for thermal & weathering properties of aggregates / Magnesium sulfate test | ΕΝ 1367-2:2010 |
| Hardened Concrete | Testing hardened concrete - Part 3: Compressive strength of test specimens (cube specimens 15cm x 15cm x15cm) | ΕΝ 12390.03:2019 |

Site of assessment: Permanent laboratory premises, 19 Emm. Papadaki Str, N. Iraklio, Athens, Greece

Approved signatories: A. Kollios, C. Tsiavos.

This scope of Accreditation replaces the previous one, dated 27.04.2023.

The Accreditation Certificate No. 1269 to ELOT EN ISO/IEC 17025:2017, is valid until 12.10.2025.

Athens,  22.02.2024

Christos Nestoras

CEO of ESYD