Hellenic Accreditation System

Annex F1/2 to the Certificate No. 1247 SCOPE of ACCREDITATION of the Testing Laboratory of METRON Energy Applications S.A. 1st party NDT laboratory

| Tested materials/ products | Types of test/ Properties to be measured | Applied Standards/ Techniques to be used |
| --- | --- | --- |
| Non destructive tests |
| Metallic Materials | 1. Magnetic particle testing by the use of portable electromagnetic equipment (yoke). Examination for surface discontinuities | EN ISO 17638: 2016 Non-destructive examination of welds – Magnetic particle testing of welds ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 7: Magnetic particle examination ASTM Ε709-21 Standard method for magnetic particle examination EN 10228-1: 2016 Non-destructive testing of steel forgings – Part 1: Magnetic particle inspection EN 1369: 2012 Founding – Magnetic particle inspection ASTM Ε1444/E1444M-22a Standard practice for magnetic particle testing |
| Metallic Materials | 2. Industrial radiographic inspection (Penetration thickness 1-90mm) | EN ISO 5579:2013 Non-destructive testing – Radiographic testing of metallic materials using film and X or gamma- rays – Basic rules ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 2: Radiographic examination ASTM E94/E94M-17 Standard guide for radiographic examination ASTM E1032-19 Standard Practice for Radiographic Examination of Weldments Using Industrial X-Ray Film ΕΝ ISO 17636-1: 2022 Non-destructive testing of welds – Radiographic testing – Part 1: X- and gamma-ray techniques with films |
| Tested materials/ products | Types of test/ Properties to be measured | Applied Standards/ Techniques to be used |
| Metallic Materials | 3. Liquid penetrant testing Examination for surface discontinuities | EN 10228-2: 2016 Non-destructive testing of steel forgings – Part 2: Penetrant testing ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 6: Liquid penetrant examination ASTM E165 / E165M – 18 Standard practice for liquid penetrant examination for general industry EN ISO 3452-1: 2021 Non-destructive testing – Penetrant testing – Part 1: General principles EN 1371-1: 2011 Founding – Liquid penetrant inspection – Part 1: Sand, gravity die and low pressure die castings. ASTM E1417 / E1417M – 21e1 Standard practice for liquid penetrant testing |
| Metallic materials | 4. Ultrasonic testing | EN ISO 16810:2014 Non-destructive testing. Ultrasonic examination. General principles ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 4: Ultrasonic examination methods for in-service inspection. Article 5: Ultrasonic examination methods for materials and fabrication ASTM E 797/E797M-21 Standard practice for measuring thickness by manual ultrasonic pulse-echo contact method EN ISO 17640:2018 Non-destructive testing of welds – Ultrasonic testing - Techniques, testing levels and assessment |
| Mechanical Tests |
| Tubing / Tanks / Pressure Vessels | 1. Hydrostatic / Pneumatic test | ASTM E1003-13 (2022) Standard Practice for Hydrostatic Leak Testing ASTM A1047/A1047M-05 (2019) Standard Test Method for Pneumatic Leak Testing of Tubing |
| Flanges | 2. Torquing test | ASME Code Β16.5: 2020 |
| Metallic materials | 3. Portable Hardness Testing by the UCI Method | ASTM A1038: 2019 |

Site of assessment: Laboratory permanent premises Dimitriou Riga 45, Magoula, Attiki, Greece

Approved signatories: I.Anastopoulos, P.Golfinopoulos

This Scope of Accreditation replaces the previous one dated March 23rd, 2021

The Accreditation Certificate No. 1247 to ELOT EN ISO/IEC 17025:2017, is valid until March 22nd, 2026.

Athens, December 12th, 2022

Christos Nestoras

CEO of ESYD