Hellenic Accreditation System

Annex F1/14 to the Certificate No. 100-7

SCOPE of ACCREDITATION of the Energy Measurements Laboratory of the Center for Renewable Energy Sources and Saving

| Materials/ Products to be tested | Types of test/ Properties to be measured | Harmonized Standard/ Applied Methods/ Techniques to be used |
| --- | --- | --- |
| Physical tests |  |  |
| Solid homogeneous building materials | Measurement of Thermal Conductivity Coefficient (λ) | ISO 8302: 1991, the entire Standard, except for § 3.2.2.3 ELΟΤ ΕΝ 12664:2001, the entire Standard, except for § 6.3.3 |
|  | Measurement of Thermal Resistance (R) |  |
| Thermal insulation products for buildings Factory made mineral wool (MW) products Factory made products of expanded polystyrene (EPS) Factory made products of extruded polystyrene foam (XPS) Factory made rigid polyurethane foam (PUR) products Factory made products of phenolic foam (PF) Factory made cellular glass (CG) products Factory made wood wool (WW) products Factory made products of expanded perlite (EPB) Factory made products of expanded cork (ICB) Factory made wood fibre (WF) products | Regulation (EU) 305/2011 System 3 ELΟΤ EN 13162: 2012+A1:2015 § 4.2.1 ELΟΤ EN 13163: 2012+A2:2016, § 4.2.1 ELΟΤ EN 13164: 2012+A1:2015, § 4.2.1 ELΟΤ EN 13165: 2012+A2:2016, § 4.2.1 ELΟΤ EN 13166: 2012+A2:2016, § 4.2.1 ELΟΤ EN 13167: 2012+A1:2015, § 4.2.1 ELΟΤ EN 13168: 2012+A1:2015, § 4.2.1 ELΟΤ EN 13169: 2012+A1:2015, § 4.2.1 ELΟΤ EN 13170: 2012+A1:2015, § 4.2.1 ELΟΤ EN 13171: 2012+A1:2015, § 4.2.1 |  |
|  | Measurement of Thermal Conductivity Coefficient (λ) | ELΟΤ ΕΝ 12667:2001, the entire Standard, except for § 6.3.3 / Guarded hot plate apparatus |
|  | Measurement of Thermal Resistance (R) |  |
| Building materials / components | Measurement of Τhermal Transmittance Coefficient | ELOT ΕΝ ISO 8990:1997 |
|  | Measurement of Thermal Resistance |  |
| Windows and doors | Regulation (EU) 305/2011 ELΟΤ EN 14351-1+Α2: 2016, § 4.12 System 3 |  |
|  | Measurement of Τhermal Transmittance Coefficient | ELOT ΕΝ ISO 12567-1:2010 / Guarded hot box apparatus |
|  | Measurement of Thermal Resistance |  |

* These Standards have been withdrawn and replaced by the corresponding versions of the 2012.

Site of assessment: Permanent laboratory premises, 19th km. Marathonos Ave., Pikermi, Attiki, Greece.

Approved signatory: Andreas Androutsopoulos.

This Scope of Accreditation replaces the previous one dated July 27th, 2022.

The Accreditation Certificate No. 100-7, to ELOT EN ISO/IEC 17025: 2017, is valid until September 23rd, 2027.

Athens, March 6th, 2023

Christos Nestoras

CEO of ESYD