Hellenic Accreditation System

Annex F1/1 to the Certificate No. 1291 SCOPE of ACCREDITATION of the Laboratory of the Newtron Technologies S.A., Aspropyrgos Business Unit

| Materials / Products to be tested | Types of test / Properties to be measured | Applied Methods / Techniques to be used |
| --- | --- | --- |
| Non Destructive Tests |
| Metallic Materials / Welds, Casting, Forgings | 1. Magnetic particle testing by the use of portable electromagnetic equipment (yoke). Examination for surface discontinuities. | EN ISO 17638: 2016 Non-destructive examination of welds – Magnetic particle testing of welds. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 7: Magnetic particle examination. ASTM E1444/E1444M-21 Standard practice for Magnetic Particle Testing for aerospace. EN 10228-1: 2016 Non-destructive testing of steel forgings – Part 1: Magnetic particle inspection. EN 1369: 2012 Founding – Magnetic particle inspection. |
| Metallic Materials / Welds, Casting, Forgings | 2. Liquid penetrant testing. Examination for surface discontinuities. | EN ISO 3452-1: 2021 Non-destructive testing – Penetrant testing – Part 1: General principles. ASTM E1417/E1417M-21e1 Standard practice for Liquid Penetrant Testing. ASTM E165/E165M-18 Standard practice for Liquid Penetrant Testing for General Industry. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 6: Liquid penetrant examination. EN 10228-2: 2016 Non-destructive testing of steel forgings – Part 2: Penetrant testing. |
| Metallic materials / Welds | 3. Ultrasonic testing Examination for discontinuities and thickness measurement. | ISO 16810: 2012 Non-destructive testing. Ultrasonic testing. General principles. EN ISO 17640: 2018 Non-destructive testing of welds – Ultrasonic testing - Techniques, testing levels and assessment. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 4: Ultrasonic examination methods for in-service inspection. Article 5: Ultrasonic examination methods for materials and fabrication. ASTM E797/E797M-21 Standard practice for measuring thickness by manual ultrasonic pulse – echo contact method. |
| Metallic materials / Welds | 4. Ultrasonic testing Examination for discontinuities by the Phased Array Method. | EN ISO 13588: 2019 Non-destructive testing of welds. Ultrasonic testing. Use of automated phased array technology. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 23, Appendix III: Phased Array Method. |
| Metallic materials / Welds | 5. Examination for discontinuities by the Radiographic Method. | EN ISO 5579: 2013 Non-destructive testing. Radiographic testing of metallic materials using film and X- or gamma rays. Basic rules. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 2: Radiographic examination. ASTM E94/E94M-17 Standard guide for radiographic examination using industrial radiographic films. ASTM E1032-19 Standard practice for radiographic examination of weldments using industrial x-ray films. ΕΝ ISO 17636-1: 2013 Non-destructive testing of welds – Radiographic testing – Part 1: X- and gamma-ray techniques with films. ΕΝ ISO 17636-2: 2013 Non-destructive testing of welds – Radiographic testing – Part 2: X- and gamma-ray techniques with digital detectors. |
| Metallic materials / Welds | 6. Visual Examination | EN ISO 17637: 2016 Non-destructive testing of welds – Visual testing of fusion welded joints. EN ISO 5817: 2014 Welding. Fusion-welded joints in steel, nickel, titanium and their alloys (beam welding excluded). Quality levels for imperfections. ASME Boiler and pressure vessel code - Section V: 2021 – Non-destructive examination. Article 9: Visual examination. |
| Mechanical Tests |
| Metallic materials | 1. Portable Hardness testing – UCI Method | ASTM A1038-19 Standard test methods for portable Hardness testing by UCI Method. |

Site of assessment: Laboratory permanent premises, Aspropyrgos, 19300 Greece

Approved signatories: Anastasios Archontopoulos, Ilias Zacharakis, Emmanouil Antonakakis, Eustratios Kapetanas, Vasilios Mperdelis, Andreas Sotiropoulos, Luigi-Giovanni Spiliotopoulos

The Accreditation Certificate No.1291 to ELOT EN ISO/IEC 17025:2017, is valid until April 10th, 2026.

Athens, April 11th, 2022

Christos Nestoras

CEO of ESYD