Hellenic Accreditation System

Annex F1/A24 to the Certificate No. 64-8 SCOPE of ACCREDITATION of the Testing Laboratories of the Materials Industrial Research and Technology Center S.A. (MIRTEC S.A.) VOLOS

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Metallic products Welded joints. Fusion weld joints in metallic materials to and above 8mm thick. Martensitic or ferritic steel forgings. Full penetration welded joints in ferritic steels. Gas and Arc welding in carbon and low-alloy steel piping. Cast steels. Welded joints. | 1. Ultrasonic examination using the pulse echo technique | EN ISO 16810:2014 ASME V Art. 4: 2021 ASME V Art. 5: 2021 ELOT ΕΝ ISO 17640: E2:2018 ΕLΟΤ ΕΝ 10228-3 Ε2: 2016 ELOT ΕΝ ISO 11666: E2:2018 API 1104: 21st Edition (Acceptance levels) ASME VIII App. 7: 2017 (Acceptance levels) ASME VIII App. 12: 2017 (Acceptance levels) |
| Metallic products Welded joints, Cast metallic materials Fusion welds of metallic materials. Gas and Arc welding in carbon and low alloy steel piping. Steel butt welds. Aluminum butt welds. Arc-welded joints in steels. Welded joints in metallic materials. Cast steels. | 2. Radiographic examination by X-Rays in Steel products up to 35mm in thickness and aluminum alloy products up to 100mm in thickness (the testing is only performed in permanent laboratory premises) | EN ISO 5579:2014 ASΤM Ε94/E94M-17 ASME V Art. 2: 2021 ELOT ΕΝ ISO 17636-1: 2013 API 1104: 21st Edition (Test method and acceptance levels) EN ISO 10675-1 Ε2: 2016 (Acceptance levels) EN ISO 10675-2 Ε2: 2018 (Acceptance levels) ELOT ΕΝ ISO 5817 E3: 2014 (Acceptance levels) ASME VIII App. 4: 2017 ASME IX QW-191.2: 2017 ASME VIII App. 7 : 2017 (Acceptance levels) ASTM E 446: 2015 (Acceptance levels) |
| Ferromagnetic materials Ferromagnetic welds. Forgings of ferromagnetic materials. Ferromagnetic cast steels. | 3. Magnetic particle inspection using magnetic particles and YOKE (Electromagnetic balance) | ASΤM Ε 709: 2017 ASME V Art. 7: 2021 ASME VIII App. 6: 2017 (Acceptance levels) ELOT ΕΝ ISO 17638 Ε2: 2016 ELOT EN ISO 23278:2015 ELOT ΕΝ ISO 5817 E3: 2014 (Acceptance levels) ELOT ΕΝ 10228-1 Ε2: 2016 ASME VIII App. 7: 2017 |
| Metallic materials Welded joints of metallic materials. Cast steels. | 4. Liquid penetrant inspection using visible and fluorescent contrast. | ASΤM Ε165/Ε165Μ-12 ELOT ΕΝ 3452.01:2021 ASME V Art. 6: 2021 ASME VIII App. 8: 2017 (Acceptance levels) ELOT EN ISO 23277 Ε2:2015 (Acceptance levels) ELOT ΕΝ ISO 5817 E3: 2014 (Acceptance levels) ELOT ΕΝ ISO 10042:2008 (Acceptance levels) ASME VIII App. 7: 2017 (Acceptance levels) |
| Metallic materials | 5. Non-destructive testing - Ultrasonic thickness measurement | ΕΛΟΤ EN ISO 16809:2019 ASTM Ε797/Ε797Μ-15 |
| Welded joints. | 1. Visual examination – Detection and evaluation of imperfections | ELOT EΝ ISO 17637: Ε2: 2017 ELΟΤ ΕΝ ΙSO 5817 Ε3: 2014 ELΟΤ ΕΝ ISO 10042: 2008 ASME V, art. 9: 2021 |
| Metallic materials. | 1. Tensile test (0-600)kN. | ELOT ΕΝ ISO 6892-1: E3:2020 (tensile strength, yield strength, percentage plastic extension at maximum force, percentage elongation after fracture) ASTM Ε8/E8M-16a (Sample dimensions) |
|  | 2. Charpy impact test. | ELOT ΕΝ ISO 148-1: E2: 2017 ELOT ΕΝ ISO 9016 E2:2012 ASTM Α370-17a (Sample dimensions) |
| Steel reinforcing bars. | 3. Bend test (at 180( angle). | ELΟΤ 1421-2,-3 E2: 2007 ΕLΟΤ ΕΝ 10080: 2005 |
|  | 4. Fatigue strength. | ΕLΟΤ ΕΝ 10080:2005, ELΟΤ 1421-2,-3 E2: 2007 |
|  | 5. Surface geometry of ribbed or indented steel. | ΕLΟΤ ΕΝ 10080: 2005, ELΟΤ 1421-2,-3 E2: 2007 |
| Welded joints. Gas and Arc welding in carbon and low alloy steel piping. Welded joints in pipes and plates. | 6. Bend test in metallic materials. | API 1104: 21st Edition ELOT ΕΝ ISO 5173/A1: 2012 ASME IX, QW 162: 2010 |
| Carbon and low-alloy steel. | C, Si, Mn, P, S, Cr, Ni, Mo, V, Cu, Al, Co, Nb, Ti, Sn, N | ASTM E 415-21 |
| Stainless steel. | C, Si, Mn, P, S, Cr, Ni, Mo, Cu | ASTM E 1086: 2022 |
| Aluminum and aluminum-alloys. | Si, Fe, Cu, Mn, Mg, Zn, Ni, Cr, Pb, Sn, Ti | ΕΝ 14726: 2006 |
| Copper alloys. | Sn, Pb, Zn, P, Mn, Fe, Ni, Si, Al, Cu | EN 15079: 2015 |
| Metallic products | Corrosion (salt spray) tests Visual examination | ΕΝ ISO 9227:2022 |
| Fire extinguishers | 1. Corrosion (salt spray) tests | ΕΝ ISO 9227:2022 |
| Portable extinguishers Mobile extinguishers Small disposable of the aerosol type extinguishers Portable extinguishers Mobile extinguishers Small disposable of the aerosol type extinguishers | 2. Extinguishing capacity tests (dielectric constant excluded) | ΕLΟΤ EN 3-7 + Α1: 2007 ΕLΟΤ EN 1866-1: 2007 ΕLΟΤ 1066 E2: 2006 |
|  | 3. Characteristics, performance and test methods (dielectric constant excluded) | ΕLΟΤ EN 3-7 + Α1: 2007 ΕLΟΤ EN 1866-1: 2007 ΕLΟΤ 1066 E2: 2006 |
| Portable aerosol dispensers for fire extinguishing purposes | External Corrosion Resistance of aerosol dispensers Protective cover removal test of aerosol dispensers Internal Corrosion Resistance of aerosol dispensers Pressure and chemical stability of aerosol dispensers Impact Resistance test of aerosol dispensers Resistance to shocks and mechanical damage of aerosol dispensers | ΕΝ 16856: 2020 §5.3.1 ΕΝ 16856: 2020 §5.1.7 – 5.1.8 ΕΝ 16856: 2020 §5.3.2 ΕΝ 16856: 2020 §5.3.3 ΕΝ 16856: 2020 §5.4 ΕΝ 16856: 2020 §5.5 |
| Aerosol canisters for extinguishing purposes | Pressure test of aerosol dispensers Burst Pressure test of aerosol dispensers | ΕΝ 16856: 2020 §5.6 ΕΝ 16856: 2020 §5.7 |
| Portable aerosol dispensers for fire extinguishing purposes Fire extinguishing performance rating — Ratings | Filling requirements and media tolerance of aerosol dispensers Filling pressure Maximum developed pressure Duration of discharge of aerosol dispensers Minimum discharge of contents of aerosol dispensers Retention of charge following partial discharge of aerosol dispensers Solid fuel extinguishing test (Type A fire) Liquid Fuel Extinguishing Test (Type B Fire) Fuel oil extinguishing test (Fire type F) Calculation test for effective throw of aerosol dispensers of aerosol dispensers Marking and color control of aerosol dispensers | ΕΝ 16856: 2020 §6.1 ΕΝ 16856: 2020 § 6.2 ± 0,5 bar από την πίεση λειτουργίας στους 20οC ΕΝ 16856: 2020 §6.3 ΕΝ 16856: 2020 §7.2 ΕΝ 16856: 2020 §7.3 ΕΝ 16856: 2020 §7.4 ΕΝ 16856: 2020 §7.5.2 ΕΝ 16856: 2020 § 7.5.3 ΕΝ 16856 : 2020 § 7.5.4 ΕΝ 16856 : 2020 § 7.6 ΕΝ16856:2020 |

Site of assessment:   Laboratory permanent premises, A' Industrial Area, Volos, Greece.

Approved Signatories: G. Archontis, A. Stamou.

This Scope of Accreditation replaces the previous one dated October 11th, 2022.

The Accreditation Certificate No. 64-8, to ELOT EN ISO/IEC 17025:2017, is valid until 28.02.2026.

Athens, July 7th, 2023

Christos Nestoras

CEO of ESYD

# Text boxes

###### Non destructive tests

Physical tests

###### Mechanical tests

###### Chemical tests

###### Control tests for fire extinguishers