Hellenic Accreditation System

| Annex F1/26 to the Certificate No. 177-9 SCOPE of ACCREDITATION of the Testing Laboratory of PILIDIS THOMAS & Co G.P. (NDT METALS) |
| --- |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| Non-destructive tests using magnetic particles |
| Ferromagnetic materials and welds of metal plates and pipes | Magnetic particles examination and use of portable yoke. | EN ISO 17638: 2016 Non-destructive testing of welds. Magnetic particle testing ΕΛΟΤ ΕΝ 10228-1 E2: 2016 Non-destructive testing of steel forgings. Magnetic particle inspection. ASME V: 2023 Boiler and Pressure Vessel Code Non Destructive Examination Article 7: Magnetic Testing. API 1104 22nd Edition Standard Welding of Pipelines and Related Facilities. Paragraph 9.4: Magnetic Particle Testing. ASTM E3024_E3024M-22A Practice for Magnetic Particle Testing for General Industry ASTM E 709: 21 Standard Practice for Magnetic Particle Testing |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Non-destructive tests using penetrant fluids |
| Non-porous materials and constructions and welds | In situ inspection by penetrant fluids | EN ISO 3452-1: 2021 Non-destructive testing. Penetrant testing. General principles ΕΛΟΤ ΕΝ 10228-2 E2: 2016 Non-destructive testing of steel forgings. Penetrant testing. ASME V: 2023 Boiler and Pressure Vessel Code Non Destructive Examination Article 6: Penetrant testing. API 1104 22nd Edition Standard Welding of Pipelines and Related Facilities. Paragraph 9.5: Liquid Penetrant Testing. ASTM E 1417/Ε 1417Μ-21e1 Standard Practice for Liquid Penetrant Testing ASTM E 165/Ε165M-2023 Standard Practice for Liquid Penetrant Examination for General Industry. |
| Ultrasonic non-destructive tests |
| Ferromagnetic materials and welds of metal plates | Ultrasonic examination. | EN ISO 16810: 2014 Non-destructive testing. Ultrasonic testing. General principles ΕΛΟΤ ΕΝ 10228-3 E2: 2016 Non-destructive testing of steel forgings. Ultrasonic testing of ferritic or martensitic steel forgings. ΕΝ ISO 23279: 2017 Non-destructive testing of welds. Ultrasonic testing. Characterization of discontinuities in welds EN ISO 17640: 2018 Non-destructive testing of welds. Ultrasonic testing. Techniques, testing levels, and assessment ASME V: 2023 Boiler and Pressure Vessel Code Non Destructive Examination Article 4: In Service Inspection, Article 5: Inspection of Materials and Fabrications. API 1104 22nd Edition Standard Welding of Pipelines and Related Facilities. Paragraph 9.6: Ultrasonic Testing. ASTM E 797/E797M: 21 Standard Practice for Measuring Thickness by Manual Ultrasonic Pulse Echo Contact Method |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Non-destructive tests by radiographic examination |
| Metallic materials and welds | X and γ ray radiographic examination. | EN ISO 5579:2013 Non-destructive Testing. Radiographic Testing of Metallic Materials using film and x- or gamma Rays. Basic Rules. EN ISO 17636-1: 2022 Non-destructive Testing of Welds. Radiographic Testing. X- and gamma- rays techniques with film. ASME V: 2023 Boiler and Pressure Vessel Code Non Destructive Examination Article 2: Radiographic examination. API 1104 22st Edition Standard Welding of Pipelines and Related Facilities. Paragraph 9.3: Radiographic Testing. ASTM E94/E94M-22 Standard Guide for Radiographic Examination ASTM E 1032: 19 Standard Test Method Guide for Radiographic Examination of weldments |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Non-destructive tests by visual examination |
| Metallic materials and welds | Visual examination | EN ISO 17637 E2: 2017 Non-destructive testing of welds. Visual testing of fusion-welded joints. EN ISO 5817: 2023 Welding. Fusion-welded joints in steel, nickel, titanium and their alloys (beam welding excluded). Quality levels for imperfections. |
| Mechanical tests |
| Metallic materials | Tensile test: Maximum force Elongation after fracture Upper & lower yield point Fracture stress | BS EN ISO 6892-1:2019 |
| Metallic materials | Impact testing (charpy) Absorbed impact energy | EVS EN ISO 148-1:2016 |
| Weld metallic specimens | Face Bend testing (FBB) & Root Bend testing (RBB): | EVS EN ISO 5173:2023 |
| Weld metallic specimens | Transverse tensile test: - Elongation - Fracture stress Rm | BS EN ISO 4136:2022 |
| Metallurgical tests |
| Metallic materials & Welding metallic specimens | Vickers Hardness / Hardness (HV10) | EVS EN ISO 6507-1:2023 |
| Welding metallic specimens | Macroscopic Examination | EVS EN ISO 17639:2022 |

Site of assessment: Laboratory Permanent premises, Industrial Park  Neochoroudas,  54500 Neochorouda, Thessaloniki, Greece.

Approved signatories: Thomas Pilidis.

This Scope of Accreditation replaces the previous one dated March 3rd, 2023.

The Accreditation Certificate No. 177-9, to ELOT EN ISO/IEC 17025: 2017, is valid until 22.09.2024.

Athens,  February 6th, 2024

Christos Nestoras

CEO of ESYD