Hellenic Accreditation System

Annex F1A/17 to the Certificate No. 159-6 SCOPE of ACCREDITATION of the Laboratory for Non Destructive and Mechanical Tests of the “T.C.L. Co. – Test & Control Laboratories” AVRAMIDIS ELEFTHERIOS – DIPSAKIS ANTONIOS Co. (Athens Laboratory)

| Materials / Products to be tested | Types of test / Properties to be measured | Applied Methods / Techniques to be used |
| --- | --- | --- |
| Metallic materials, products and fabrications, including weldings Penetration thickness: (1 – 100) mm Metallic materials, products and fabrications, including weldings Penetration thickness: (1 – 100) mm (cont.) | Α1. Radiographic inspection using X and Gamma-rays ( IR 192 & SE 75) Α1. Radiographic inspection using X and Gamma-rays ( IR 192 & SE 75) (cont.) | EN ISO 5579: 2013 Non-destructive testing - Radiographic testing of metallic materials using film and X or gamma-rays – Basic rules |
|  |  | ELOT EN ISO 17636-1: 2013 Non-destructive testing of welds - Radiographic testing – Part 1: X- and gamma-ray techniques with films |
|  |  | EN ISO 10893-6: 2019 Non destructive testing of steel tubes. Radiographic testing of the weld seam of welded steel tubes for the detection of imperfections. |
|  |  | ASTM E94/Ε94Μ-17 Standard Guide for Radiographic examination. |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 2: Radiographic Examination. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraph 9.3 Radiographic testing |
| Weldments of metallic materials Base metal ( 8 mm | Α2. Ultrasonic testing | EN ISO 16810: 2014 Non destructive testing. Ultrasonic examination. General principles |
|  |  | BS ΕΝ ISO 11666: 2018 Non destructive testing of welds-Ultrasonic testing-Acceptance levels. |
|  |  | ELOT ΕΝ ISO 23279 Ε2: 2017 Non destructive testing of welds-Ultrasonic testing-Characterization of indications in welds. |
|  |  | BS ΕΝ ISO 17640: 2018 Non destructive testing of welds- Ultrasonic testing – Techniques, testing levels and assessment. |
|  |  | EN ISO 16827: 2014 Non destructive testing. Ultrasonic examination. Characterization and sizing of discontinuities. |
|  |  | ΕΝ ISO 10893-8: 2011 Non destructive testing of steel tubes. Automated ultrasonic testing of seamless and welded steel tubes for the detection of laminar imperfections. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraph 9.6 Ultrasonic testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 4: Ultrasonic examination methods for in-service inspection. Article 5: Ultrasonic examination methods for Materials and fabrication. |
| Metallic plates | Α3. Ultrasonic testing of plates | ELOT ΕΝ 10160: 1999 Ultrasonic testing of steel flat product of thickness equal or greater than 6mm (reflection method). Thickness ( 6 mm |
|  |  | ASTM E 797/E797M: 2015 Standard practice for measuring thickness by manual ultrasonic pulse-echo contact method. |
| Ferromagnetic materials, products and fabrications, including weldments, castings and steel forgings | Α4. Magnetic particle testing by the use of portable electromagnetic yoke Investigation for surface discontinuities | ELOT EN ISO 17638 Ε2: 2016 Non destructive examination of welds-Magnetic particle testing of welds |
|  |  | ΕΝ ISO 10893-5: 2011 Non destructive testing of steel tubes. Magnetic particle inspection of tube ends of seamless and welded ferromagnetic steel tubes for the detection of surface imperfections. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraph 9.4 magnetic particle testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 7: Magnetic particle examination |
|  |  | EN 1369: 2012 Founding- Magnetic Particle Inspection |
|  |  | ELOT EN ISO 9934-1 E3: 2017 Non destructive testing-Magnetic Particle testing-Part 1:General Principles |
|  |  | ELOT EN 10228-1 Ε2: 2016 Non destructive testing of steel forgings-Part 1: Magnetic particle inspection |
|  |  | ASTM Ε709-15 Standard method for magnetic particle examination |
| Non porous materials, products and fabrications, including weldments, castings and steel forgings Non porous materials, products and fabrications, including weldments, castings and steel forgings (cont.) | Α5. On site liquid penetrant testing Investigation for surface discontinuities Α5. On site liquid penetrant testing Investigation for surface discontinuities (cont.) | EN ISO 3452-1:2013 Non destructive testing-Penetrant testing-Part 1: General principles |
|  |  | ELOT EN ISO 23277 E2: 2015 Non destructive testing of welds – Penetrant testing of welds – Acceptance levels. |
|  |  | EN ISO 10893-4: 2011 Non destructive testing of steel tubes. Liquid penetrant inspection of seamless and welded steel tubes for the detection of surface imperfections |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraph 9.5 : Liquid penetrant testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 6: Liquid penetrant examination. |
|  |  | ELOT EN 10228-2 Ε2: 2016 Νon destructive testing of steel forgings-Part 2: Penetrant testing |
|  |  | ELOT EN 1371-1 E2: 2012 Founding – Liquid penetrant inspection- Part 1 Sand, gravity die and low pressure die castings. |
|  |  | ASTM E165 / E165M - 18 Standard Practice for Liquid Penetrant Examination of General Industry |
| Weldings of metal structures | A6. Visual testing (direct method only) | BS EN ISO 17637: 2016 Non-destructive testing of welds - Visual testing of fusion-welded joints. ELOT EN ISO 5817 E3: 2014 Fusion-welded joints in steel, nickel, titanium and their alloys (beam welding excluded) - Quality levels for imperfections. ASME V art 9: 2019 ASME IX QW194: 2019 API 1104 21st Edition § 6.4, 9.7 |
| Metallic materials and products, including weldings | Β1. Tensile testing (120-200) kN (Only elongation after fracture and tensile strength) | ELOT EN ISO 4136: 2012 Destructive tests on welds in metallic materials – Transverse Tensile Test |
|  |  | ELOT EN ISO 6892-1 Ε2: 2016 Metallic materials – Tensile testing – Part 1- Method of test at ambient temperature. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraphs 5.6.2: Tensile strength test, 5.6.3: Nick break test. |
|  |  | ASME Boiler and pressure vessel code Section IX: 2019 QW 150 Tension tests |
|  | Β2. Bend testing (0-200) kN | ELOT EN ISO 5173: 2011 ELOT EN ISO 5173/Α1: 2012 Destructive tests on welds in metallic materials – Bend tests |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraphs 5.6.4: Root & Face bend test, 5.6.5: Side – bend test |
|  |  | ASME Boiler and pressure vessel code Section IX: 2019 QW 160 Guided bend tests |

Site of assessment: Laboratory Permanent premises: Position Patima Rathiri, GR-19300 Aspropyrgos, Attiki,

Greece.

Approved signatories: A. Dipsakis.

This Scope of Accreditation replaces the previous one dated May 8th, 2018.

The Accreditation Certificate No. 159-6, to ELOT EN ISO/IEC 17025: 2017, is valid until December 6th, 2020.

Athens, June 23rd, 2020

Spyridon Podaras

CEO of ESYD

Hellenic Accreditation System

Annex F1B/15 to the Certificate No. 159-6 SCOPE of ACCREDITATION of the Laboratory for Non Destructive and Mechanical Tests of the “T.C.L. Co. – Test & Control Laboratories” AVRAMIDIS ELEFTHERIOS – DIPSAKIS ANTONIOS Co. (Laboratory in Thessaloniki)

| Materials / Products to be tested | Types of test / Properties to be measured | Applied Methods / Techniques to be used |
| --- | --- | --- |
| Metallic materials, products and fabrications, including weldings Penetration thickness: (1 – 100) mm Metallic materials, products and fabrications, including weldings Penetration thickness: (1 –100) mm (cont.) | Α1. Radiographic inspection using X and Gamma-rays ( IR 192 & SE 75) Α1. Radiographic inspection using X and Gamma-rays ( IR 192 & SE 75) (cont.) | EN ISO 5579: 2013 Non-destructive testing - Radiographic testing of metallic materials using film and X or gamma-rays – Basic rules |
|  |  | ELOT EN ISO 17636-1: 2013 Non-destructive testing of welds - Radiographic testing – Part 1: X- and gamma-ray technique with films |
|  |  | EN ISO 10893-6: 2019 Non destructive testing of steel tubes. Radiographic testing of the weld seam of welded steel tubes for the detection of imperfections. |
|  |  | ASTM E 94/E94M-17 Standard Guide for Radiographic examination. |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 2: Radiographic Examination. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraph 9.3 Radiographic testing |
| Weldments of metallic materials Base metal ( 8 mm Weldments of metallic materials Base metal ( 8 mm (cont.) | Α2. Ultrasonic testing Α2. Ultrasonic testing (cont.) | EN ISO 16810: 2014 Non destructive testing. Ultrasonic examination. General principles |
|  |  | BS ΕΝ ISO 11666: 2018 Non destructive testing of welds-Ultrasonic testing-Acceptance levels. |
|  |  | ELOT ΕΝ ISO 23279 Ε2: 2017 Non destructive testing of welds-Ultrasonic testing-Characterization of indications in welds. |
|  |  | BS ΕΝ ISO 17640: 2018 Non destructive testing of welds- Ultrasonic testing – Techniques, testing levels and assessment. |
|  |  | EN ISO 16827: 2014 Non destructive testing. Ultrasonic examination. Characterization and sizing of discontinuities. |
|  |  | ΕΝ ISO 10893-8: 2011 Non destructive testing of steel tubes. Automated ultrasonic testing of seamless and welded steel tubes for the detection of laminar imperfections. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraph 9.6 Ultrasonic testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 4: Ultrasonic examination methods for in-service inspection. Article 5: Ultrasonic examination methods for Materials and fabrication. |
| Metallic plates | Α3. Ultrasonic testing of plates | ELOT ΕΝ 10160: 1999 Ultrasonic testing of steel flat product of thickness equal or greater than 6mm (reflection method). Thickness ( 6 mm |
|  |  | ASTM E 797/E797M: 2015 Standard practice for measuring thickness by manual ultrasonic pulse-echo contact method. |
| Ferromagnetic materials, products and fabrications, including weldments, castings and steel forgings Ferromagnetic materials, products and fabrications, including weldments, castings and steel forgings (cont.) | Α4. Magnetic particle testing by the use of portable electromagnetic yoke Investigation for surface discontinuities Α4. Magnetic particle testing by the use of portable electromagnetic yoke Investigation for surface discontinuities (cont.) | ELOT EN ISO 17638 Ε2: 2016 Non destructive examination of welds-Magnetic particle testing of welds |
|  |  | ΕΝ ISO 10893-5: 2011 Non destructive testing of steel tubes. Magnetic particle inspection of tube ends of seamless and welded ferromagnetic steel tubes for the detection of surface imperfections. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraph 9.4 magnetic particle testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 7: Magnetic particle examination |
|  |  | EN 1369: 2012 Founding- Magnetic Particle Inspection |
|  |  | ELOT EN ISO 9934-1 E3: 2017 Non destructive testing-Magnetic Particle testing-Part 1:General Principles |
|  |  | ELOT EN 10228-1 Ε2: 2016 Non destructive testing of steel forgings-Part 1: Magnetic particle inspection |
|  |  | ASTM Ε709-15 Standard method for magnetic particle examination |
| Non porous materials, products and fabrications, including weldments, castings and steel forgings | Α5. On site liquid penetrant testing Investigation for surface discontinuities | EN ISO 3452-1: 2013 Non destructive testing-Penetrant testing-Part 1: General principles |
|  |  | ELOT EN ISO 23277 E2: 2015 Non destructive testing of welds – Penetrant testing of welds – Acceptance levels. |
|  |  | EN ISO 10893-4: 2011 Non destructive testing of steel tubes. Liquid penetrant inspection of seamless and welded steel tubes for the detection of surface imperfections |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraph 9.5 : Liquid penetrant testing |
|  |  | ASME Boiler and pressure vessel code Section V: 2019 Non Destructive Examination Article 6: Liquid penetrant examination. |
|  |  | ELOT EN 10228-2 Ε2: 2016 Νon destructive testing of steel forgings-Part 2: Penetrant testing |
|  |  | ELOT EN 1371-1 E2: 2012 Founding – Liquid penetrant inspection- Part 1 Sand, gravity die and low pressure die castings. |
|  |  | ASTM E165 / E165M - 18 Standard Practice for Liquid Penetrant Examination of General Industry |
| Weldings of metal structures | A6. Visual testing (direct method only) | BS EN ISO 17637: 2016 Non-destructive testing of welds - Visual testing of fusion-welded joints. EN ISO 5817 E3: 2014 Fusion-welded joints in steel, nickel, titanium and their alloys (beam welding excluded) - Quality levels for imperfections. ASME V art 9: 2019 ASME IX QW194: 2019 API 1104 21st Edition § 6.4, 9.7 |
| Metallic materials and products, including weldings | Β1. Tensile testing (0-400) kN (Only elongation after fracture and tensile strength). | EN ISO 4136: 2012 Destructive tests on welds in metallic materials – Transverse Tensile Test |
|  |  | ELOT EN ISO 6892-1 Ε2: 2016 Metallic materials – Tensile testing – Part 1- Method of test at ambient temperature. |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities Paragraphs 5.6.2: Tensile strength test, 5.6.3: Nick break test |
|  |  | ASME Boiler and pressure vessel code Section IX : 2019 QW 150 Tension tests |
|  | Β2. Bend testing (0-400) kN | ELOT EN ISO 5173: 2011 ELOT EN ISO 5173/Α1: 2012 Destructive tests on welds in metallic materials – Bend tests |
|  |  | API 1104 21st Edition Welding of pipelines and related facilities. Paragraphs 5.6.4: Root & Face bend test, 5.6.5: Side – bend test |
|  |  | ASME Boiler and pressure vessel code Section IX: 2019 QW 160 Guided bend tests |

Site of assessment: Laboratory Permanent premises: Agrotemachio 579, Municipality of Echedoros, Thessaloniki, Greece.

Approved signatories: El. Avramidis.

This Scope of Accreditation replaces the previous one dated , May 8th, 2018.

The Accreditation Certificate No. 159-6, to ELOT EN ISO/IEC 17025: 2017, is valid until December 6th , 2020, according ESYD decision.

Athens, June 23rd, 2020

Spyridon Podaras

CEO of ESYD

# Text boxes

A' Non destructive tests

B' Mechanical tests

A' Non destructive tests

B' Mechanical tests